Exam 4  —  to supplement Quiz 8a-8b and 8c

Addition Polymers — Heads and Tails

The “spatial rhythm” is defined (and can be seen) in each name:

Head-to-Tail , Head-to-Tail              Head-to-Head , Tail-to-Tail

1		     -	    3		-		   	    1		 2		 -		 -

Page 379 suggests “arbitrarily thinking of” the carbon-with-H as Head, but this is arbitrary.  To make the rhythms 1-3- (not -2-4) and 12- - (not - -34),  I prefer to define C-with-the-large-group (CH3 , Cl,     ) as Head because the names — “Head-to-Tail...” and “Head-to-Head...” — are fixed by tradition, not by me.

Big Six (p 378):  know structures & names, properties-and-uses.

Writing Condensation Reactions — a step-by-step strategy
uses Steps (0, 1, 2, 3) analogous to Addition Polymerization.
Step 0:  Translate from words (formic acid,...) into structures.

Step 1a:  RED - find atoms that leave:  OH of COOH, H of OH.
	BLUE - find atoms that lose bonds:  C of COOH, O of OH.
	BLUE - on right side, bond C (of C=O) with O (of OH), and
	BLACK - copy all non-Red/Blue atoms from left to right.
	RED - combine “lost”  OH and H to form HOH (i.e. H2O).
For ester-reaction, stop here;  for polyester-reaction, do 1b-2-3.
Step 1b:  draw brackets for repeating-unit ;   remove remaining
	Red-atoms (OH, H) so you can draw bonds-across-brackets.
Step 2:  n di-acids + n di-alcohols ( n repeating-units,  2n H2O.
Step 3:  For ester or polyester,  H+ (a catalyst) over-the-arrow.

• Use same steps if alcohol (-OH) is replaced by amine (-NH2);
replace H (of OH) by H (of NH2), and O (of OH) by N (of NH2);
and product (ester or polyester) is now amide or polyamide.

Later (after Exam 4, so ignore it now!) — for Quiz 9,
 • Use same steps if di-acid/di-amine (for polyamide) is replaced by amino acids (for polypeptide);   the main differences are the monomer & repeating unit (both have an R-group that can vary), and for Step 2 only n H2O is produced, instead of 2n.

This handout is for Exam 4, so why does it include ideas from after it?    To emphasize the unity of ideas & chemistry;  a wide range of applications – using condensation reactions in industry and biology – are minor variations on the same basic themes.

Polymerization  —  What is required?

To form a polymer, monomers must react to-Left and to-Right.
For addition polymer, L-and-R happens with C=C of alkene.
For polyester, use di-acid (L, R) plus di-alcohol (L, R);
for polyamide, use di-acid (L, R) plus di-amine (L, R),

and later, on Quiz 9,
for polypeptide, use amino acids (amine on L, acid on R).
For triglyceride (a non-polymer), use 3 acids plus tri-alcohol.

Structures of Monomers for:

addition (p 378 shows similarity of monomers for polyethylene, 	polypropylene,  polyvinyl chloride,  polystyrene;

polyester: PolyEthylene Terephthalic Ester  (PETE, aka PET) ;
	p 378:  ethylene glycol is 2-C di-alcohol with 1 on each C ;
	terephthalic acid [ph,th] is benzene with symmetric di-acid).

polyamides: Nylon-6,6 (p 386, 6 C in di-acid and di-alcohol),
	Kevlar (p 387, benzene with symmetric di-acid & di-amine).

and later, analogous applications of these ideas for Quiz 9,

polypeptides:  variety of Amino Acids (amine on left end, 	carboxylic acid on right end) with differing R-groups.

triglycerides (fats/oils) non-polymer:   glycerol, 3-C tri-alcohol  (p 354) plus 3 fatty acids with variety as explained on 452-461,  where one factor is saturated (no C=C) vs unsaturated (w C=C).

Catalyst (over-the-arrow) speeds up reaction but is not reactant or product in rxn-equation.    In rxns:   R• for addition polymers,  
H+ for condensation (ester & polyester, amide & polyamide, and later – after Exam 4 – to make polypeptides and triglycerides).
For other reactions (catalytic cracking, hydrocracking, adding H across C=Cs), in Chem 108 it’s just an undefined “catalyst”.

Hydrogenation Reaction:   C=C   + H2 —(catalyst)(   CH-CH

• Polysaccharides dissolve in water (very polar) due to their functional groups — ethers (polar) and alcohols (very polar) — but are non-electrolytes, don’t form ions or conduct electricity.       • flowchart in Slide 38 (Lec 33) is a great overview, showing monosaccharides (glucose, fructose), disaccharides (sucrose,...), and polysaccharides (starch, cellulose) – with 1, 2, n monomers.

• Humans more easily digest disaccharides or polysaccharides with a-linkages (rings on ≈ same plane), not b-linkages (rings on different planes), Slides 34-40:  maltose (a) vs lactose (b), starch (a) vs cellulose (b).

• HFCS (glucose, fructose) vs sucrose (glucose-and-fructose).
 	    mixture of monosaccharides			     disaccharide

Energy-Math for Energy Lab:  Know calculations from E-Lab
and in Exam 3 of 2011 (Part 4, #4), Exam 4 of 2012 (Part 2, #4):
Heat Absorbed = (__ g H2O)(Tf-T1 deg)(4.184 J/g-deg) = __ J ;
Exp Heat of Rxn = (__ Abs-Heat in J) /__ g fuel) = J / g of fuel ;
find Efficiency (p 11-5); use Efficiency (p 11-4) to get corrected
Heat of Rxn = __ J / g fuel,  and (1000 J = 1 kJ) in __ kJ / g fuel.